ARDON®Smart Grip

ACCURATE HANDLING IN DRY ENVIRONMENT WITH EXTRA GRIP

TECHNICAL DATA

ACCURATE HANDLING IN DRY ENVIRONMENT WITH EXTRA GRIP

SIZE(S)

UNIT

PACKING

Units in carton

Units in polybag

Retail packaging

120 pairs

12 pairs

sales label

TECHNICAL DATA

ARDON®Smart Grip

| DIMENSIONS | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Carton H x W x D (cm) | - | - | 46x25x26 | 46x26x30 | 46x26x30 | 46x28x32 | 46x28x32 | - |
| Carton (cbm) | - | - | 0,0300 | 0,0359 | 0,0359 | 0,0412 | 0,0412 | - |

| WEIGHT | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Carton (kg) | - | - | 5,50 | 5,90 | 6,50 | 6,90 | 7,40 | - |
| Unit (g) | - | - | 35,0 | 38,0 | 43,0 | 46,0 | 50,0 | - |

DESCRIPTION

Fine nylon knit dipped in durable nitrile microfoam with anti-slip finish.

| Size chart (cm) | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| total length (A) | - | - | 22,0 | 23,0 | 24,0 | 25,0 | 26,0 | - |
| cuff length (B) | - | - | 7,20 | 7,40 | 7,60 | 7,80 | 8,00 | - |
| cuff width (C) | - | - | 7,40 | 7,60 | 7,80 | 8,00 | 8,20 | - |
| palm width (D) | - | - | 9,00 | 9,50 | 10,6 | 11,1 | 11,6 | - |
| Tolerance (A) ± 1,00 (cm) |  |  | Tolerance (C) ± 0,70 (cm) |  |  |  |  |  |
| Tolerance (B) ± 0,70 (cm) |  |  | Tolerance (D) ± 0,70 (cm) |  |  |  |  |  |

15G nylon, lycra (black)

nitrile microfoam (black) with antislip “A“ patterned finish

±1,1 mm (in palm)

7 / S – 11 / 2XL

pair

MATERIAL

Lining

Coating

Thickness

A8024

CODE

# STANDARDS

# (EU) 2016/425

EN ISO 21420:2020           Protective gloves – general requirements and test methods

EN 388:2016 + A1:2018 Protective gloves against mechanical risks

| PROTECTION LEVELS |  |  |  |
| --- | --- | --- | --- |
| MECHANICAL RISKS | LVL | score | unit |
| abrasion resistance | 4 | > 8.000 | cycles |
| cut resistance | 1 | 1,2 – 2,5 | index |
| tearing resistance | 3 | 50 – 75 | N |
| puncture resistance | 1 | 20 – 60 | N |
| cut resistance acc. to ISO | A | 2 – 5 | N |

EN 407:2020		Protective gloves against heat or flame

| PROTECTION LEVELS |  |  |  |
| --- | --- | --- | --- |
| THERMAL RISKS | LVL | score |  |  |
| resistance to burning | X | not measured |  |  |
| resistance to contact heat | 1 | 100°C for 15s |  |  |
| resistance to convectional heat | X | not measured |  |  |
| resistance to radiant heat | X | not measured |  |  |
| resistance to small drops of molten metals | X | not measured |  |  |
| resistance to large drops of molten metals | X | not measured |  |  |

SPECIAL FEATURES

- “A“ shaped nitrile antislip coating on palm and fingers for safer and softer grip

- fine 15 gauge liner

- hem free finish

- every size with different hem colour

- ARDON® design:

▪ reflective manufacturer's logo

▪ each pair retail ready

- clean industrial look

TECHNICAL DATA

|  | EAN | HEM COLOR |
| --- | --- | --- |
| Retail packaging (with sales label) |  |  |
| A8024/07-SPE | 8592390180803 | yellow |
| A8024/08-SPE | 8592390180810 | green |
| A8024/09-SPE | 8592390180827 | orange |
| A8024/10-SPE | 8592390180834 | blue |
| A8024/11-SPE | 8592390180841 | red |

TECHNICAL DATA

TECHNICAL DATA